## Slide 1
Article
Published: 27 January 2022
A photosensitizer–polyoxometalate dyad that enables the decoupling of light and dark reactions for delayed on-demand solar hydrogen production
Sebastian Amthor,
Sebastian Knoll,
Magdalena Heiland,
Linda Zedler,
Chunyu Li,
Djawed Nauroozi,
Willi Tobaschus,
Alexander K. Mengele,
Montaha Anjass,
Ulrich S. Schubert,
Benjamin Dietzek-Ivanšić,
Sven Rau &
Carsten Streb
Nature Chemistry volume 14, pages321–327 (2022)

## Slide 3
Fig. 1: Schematic illustration of the coupled light and dark reaction.

## Slide 4
Fig. 2: Synthesis and spectroscopic properties of PS-POM.
a, Synthesis of PS-POM by reaction of the trimethylsilyl-phosphonate-functionalized Ru photosensitizer 1a with the lacunary Dawson anion 2, leading to the phosphonate-mediated covalent attachment of 1a to 2. Colour scheme: W, deep blue; O, red; P, green, yellow, light blue. r.t., room temperature; DCM, dichloromethane. b, UV-vis spectrum of PS-POM, 1 and 2, showing that the PS absorption features are retained. c, Steady-state emission spectroscopy showing the emission quenching of PS-POM and the intermolecular references (1 and 2, 2:1 molar ratio). The high quenching efficiency in PS-POM indicates strong electronic coupling between the PS and POM components. Conditions: water-free, de-aerated DMF; PS-POM (3.2 µM); PS 1 (6.4 µM); POM 2 (3.2 µM). d, Emission decay profiles of PS-POM (top) and reference 1 (bottom), measured by time-correlated single-photon counting (in DMF; excitation wavelength λexcitation = 470 nm). The data support strong electronic coupling between PS and POM, indicated by the steady-state emission spectroscopy shown in c. e, 31P NMR spectrum of PS-POM in d6-DMSO (deuterated dimethyl sulfoxide) at room temperature; colour codes correspond to the phosphorus colour labels in a, indicating the presence of three distinct chemical environments for phosphorous in PS-POM.

## Slide 5
Fig. 3: Irradiation stability assays for PS-POM and the POM-free PS reference system.
a, UV-vis spectral changes of PS-POM (2.9 μM), showing that virtually no changes to the visible-light absorption are observed over the whole irradiation period (72 h). b, UV-vis spectral changes of the reference PS 1 (5.8 μM), showing major spectral changes under irradiation, indicative of (partial) PS degradation by ligand exchange. Conditions: solvent, DMF (water-free, de-aerated); irradiation using a monochromatic LED (λmax = 470 nm, Pnominal ≈ 40 mW cm−2); tirradiation = 72 h.

## Slide 6
Fig. 4: Photophysical properties of PS-POM.
a, Transient absorption spectra at selected delay times. b, Transient kinetics at key wavelengths. c, Spectral changes associated with each kinetic process (decay-associated spectra) for PS-POM (0.3 mM in DMF), pumped at 400 nm. Upon excitation of the MLCT transitions in the PS unit, a RuIII–bpy•– species is formed within 3 ps (τ1), which shows distinct spectral features of the reduced bpy•– ligand (also Supplementary Fig. 27). The transient absorption spectrum at 12 ps (τ2) displays a broad absorption band above 600 nm, due to the characteristic IVCT absorption of the reduced POM in the charge-separated state. Subsequently, the charge-separated state decays to the ground state with a characteristic time constant of 90 ps (τ3). ΔAbs, change in absorbance; Inf., infinite component.

## Slide 7
Fig. 5: Spectral evolution of PS-POM upon photoreduction and acid addition.
a, UV-vis spectral changes of PS-POM (9 μM) upon irradiation using a monochromatic LED (λmax = 470 nm, Pnominal ≈ 40 mW cm−2) in the presence of a sacrificial electron donor (TEOA, 60 mM, 6,700 equiv.); the data show that under the given conditions, electron transfer and storage on the POM unit is possible, indicated by the characteristic, broad IVCT absorption band centred at 650 nm. b, Normalized UV-vis spectral changes of PS-POM (9 μM) upon addition of a proton source (H2SO4, 100 mM, 11,000 equiv.), showing the virtually instantaneous electron release by reaction of PS-POM with protons, resulting in H2 formation (confirmed by gas chromatography). h, Planck constant; v, light frequency; hv, light energy / irradiation, i.e., that this reaction is light-driven; t-acid-add, time after acid-addition.

## Slide 8
Fig. 6: Delayed on-demand hydrogen production.
a, Time-dependent UV-vis spectroscopic analysis of the absorption maximum at 650 nm during charging (Step 1, beginning at arrow), storage (Step 2) and discharging (Step 3, beginning at arrow), highlighting the light-induced accumulation of electrons on the POM unit as well as their release by reaction with a proton source. Conditions: solvent, water-free, de-aerated DMF; irradiation using a monochromatic LED (λmax = 470 nm, Pnominal ≈ 40 mW cm−2); proton donor, H2SO4 in DMF (4.0 M); [PS-POM] = 9 μM; sacrificial electron donor, TEOA (60 mM, 6,700 equiv.). TEOA was chosen to facilitate observation of the reduction process due to the slower PS-POM/TEOA reduction kinetics compared with other electron donors. b, Simplified energy scheme showing the energies and transitions between different experimentally observed intermediates of the on-demand hydrogen production experiment (Supplementary Section 7 for details) * marks the photoexcited system. c, Schematic illustration of the stepwise charging (Step 1), storage (Step 2) and discharging (Step 3) of the PS-POM solution, summarizing the light-dependent and light-independent reactions studied for PS-POM. Δt, delay time.