## Slide 1
View of a (001) sheet with two kinds of pores, A and B, in NENU-n (n = 1−6). The Cu-BTC framework and Keggin polyanions
are represented by wireframe and polyhedral models. Blue, red, and gray represent Cu, O, and C, respectively.
DOI: (10.1021/ja807357r)

## Slide 2
Components of the crystal structures of NENU-n (n = 1−6): (a) a cube of five truncated-octahedral cages sharing square faces;
(b) the pore A accommodating the Keggin polyanion, Cu2-cluster (blue polyhedra), Keggin polyanion (red polyhedra), C (gray),
and O (red). All H atoms and solvent molecules are omitted for clarity.
DOI: (10.1021/ja807357r)

## Slide 3
Results for the hydrolysis of ester in the presence of NENU-3a: (a) methyl acetate; (b) ethyl acetate; (c) methyl benzoate;
(d) ethyl benzoate; and (e) 4-methyl-phenyl propionate. The reactions were performed with 5 wt% 30 mL aqueous solution
for (a) and (b) at 60 °C and 2 wt% 30 mL aqueous solution for (c)−(e) at 80 °C, respectively; catalyst weight 0.20 g; reaction time 5 h.
DOI: (10.1021/ja807357r)